## Slide 1
Future Opportunities for Ultralight Materials and Structures
Lattice-based materials and structures
Haydn Wadley
University of Virginia
Charlottesville, Va

## Slide 2
Examples of cellular structures
10mm
10mm
Examples of metallic lattices

## Slide 3: Multiscale metallic metamaterials --- across over 7 orders of magnitude in length-scale
Zheng et al., Nature Materials, 2016 In Press
LED Projection Micro Stereo-lithography

## Slide 4
A.G. Evans, J.W. Hutchinson, N.A. Fleck, M.F. Ashby, H.N.G. Wadley, The topological design of multifunctional cellular metals, Progress in Materials Science, Volume 46, Issues 3–4, 2001, 309–327
Sandwich Panel Weight Minimization Concepts
Foam core weight
minimization
Core comparisons during panel bending
Haydn N.G. Wadley, Norman A. Fleck, Anthony G. Evans, Fabrication and structural performance of periodic cellular metal sandwich structures, Composites Science and Technology, Volume 63, Issue 16, 2003, 2331–2343
,
Failure loci
Load index
Transverse shear (per unit width)
Bending moment
(per unit width)
Weight index
Weight(per unit width)
Density
Characteristic length = M/V
(related to L)
Maximize core moduli, and strength, minimize core density and optimize topology

## Slide 5
Voigt (anisotropic) bound
Elastic Modulus –Density Space White Space
Highest possible bound was calculated by Voigt for anisotropic materials/structures (honeycomb).
Hashin and Shtrikman investigated bounds for elastic materials. For 3D isotropic systems these are below the Voigt (iso-strain) bound.
Lattices we are interested in (e.g. octet truss) are almost isotropic and provide multifunctionality.
Octet truss
H-S upper bound
Bend-dominated structures
Stretching structures
V.S. Deshpande, N.A. Fleck, M.F. Ashby, Effective properties of the octet-truss lattice material, Journal of the Mechanics and Physics of Solids, Volume 49, Issue 8, 2001, 1747–1769

## Slide 6
An octet-truss lattice constructed by the 3D packing of unit cells.
Each node within the octet lattice lies at the intersection of 12 struts.
The octet truss lattice
A unit cell of the face centered cubic crystal symmetry octet-truss lattice.
A central octahedral cell (with 12 struts) bounded by 8 edge tetrahedrons.
Almost isotropic
A stretch dominated structure

## Slide 7
Topology Design and Material Selection Enables Bound Limited Stiffness
Jonathan Burger, Robert McMeeking, Haydn Wadley (submitted, 2016)

## Slide 8
Opportunities in Strength –Density Space
Octet truss bound
Perhaps a >10X opportunity if we can make lattices from ultra-high strength, low density materials?
III
II
I
II
final
t = 0.00000 s
t = 450.00002 s
t = 450.00014 s
t = 450.00028 s
I
t = 450.07576 s
III
IV
IV
Core strain, c
0.00
0.01
0.02
0.03
0.04
Compressive stress, c (MPa)
0
250
150
200
50
100
TMC Compression
The failure initiating at III and ending at IV propagates in about 140 microseconds (~ 200 m/s).
5 mm
But beware of fracture as we take away plasticity

## Slide 9
Strength of a single layered pyramidal lattice
plastic yield control
Design of stretch dominated octet lattice structures
To maximize compressive strength
At lower density, compressed trusses buckle
elastic
inelastic
maximize sy, Es, Et, k and I
w
Strength of an octet lattice
2/3: since only out of plane trusses directly support out of plane load
Deshpande, Fleck, Ashby JMPS 2001
Eq (1)
Substitute scr, for sy in Eq (1)

## Slide 10
The "snap-fit" truss fabrication and assembly method for making Ti-6Al-4V octet-truss lattice
“Snap-fit” octet lattices from high specific strength materials
Retains a/b high specific strength microstructure, scalable.
Used for metal alloys, composites and extendable to ceramics
Relative density, of the snap-fit octet-truss lattice:
6(t/l)2 “ideal” octet as node volume→0
l

## Slide 11
A Ti-6Al-4V octet-truss lattice compression specimen with a relative density of 4.6%.
40Ti-20Cu-20Ni-20Zr (wt.%) braze alloy (900oC, 30min)

## Slide 12
Cauchy stress- strain response of
Ti-6Al-4V alloy
Mechanical responses
Tangent modulus (MPa)
Compressive stress strain response of octet lattices
Failure mechanism of a compressed lattice with = 4.6%
Inelastic truss buckling develops as the total strain, ε, increased

## Slide 13
Material property charts for the snap-fit Ti-6Al-4V octet lattices

## Slide 14
FDA predictions of the fracture toughness of brittle 2D lattices
2
strut
Micro-architectured materials: past, present and future, Fleck, Deshpande, Ashby, Proc Roy Soc 2010.
d= ½ (Kagome), 1 (triangulated) or 2 (hexagonal honeycomb)

## Slide 15
ASTM E1820 − 13
Measure J.
Fracture toughness of octet lattice structures
Effect of relative density
Effect of strut length

## Slide 16
Fracture toughness and compressive strength map for materials of similar density
How can we further increase the specific strength of lattices ?
Metal bonded ceramics
.
α =0.5
d= unity

## Slide 17
Some thoughts for discussion

## Slide 18
Composite (CFRP) octet truss lattices
(vinyl ester matrix: shear strength = 20 MPa)
tension
compression
g Y is the shear strain and k shear strength of rigid-ideally plastic matrix ϕ is the fiber misalignment angle (~2o) and G the shear modulus.
“Stubby” composite struts fail in compression by plastic fiber micro-buckling (Budiansky/Fleck).
Matrix | Shear strength (MPa) | Compressive strength (GPa)
Al 7074 T6 | 350 | 9.5
Ti-6Al-4V | 550 | 15
Microbuckling of Nextel610 fiber-Al2Cu lattice
Future carbon fiber

## Slide 19: SPS system (10 kA pulses, 10 ton pressure, 10 minutes)
New Processes for Rapid Composite Synthesis and Consolidation

## Slide 20
15 mm
New Process Technologies for Rapid Synthesis and Consolidation

## Slide 21
Microstructure and mechanical properties of SHS 85 vol %TiC + 15 vol% NiMo
Core rim structure of TiC arises from diffusion of Mo into surface of the carbide
Property | Symbol | As-received value | Post HIP value
Elastic modulus | E | 383 GPa | 378 GPa
Shear modulus | G | 155 GPa | 154 GPa
Poisson’s ratio | υ | 0.23 | 0.22
Vickers microhardness | HV | 1120±170 HV | 1570 ± 230 HV
Compressive Yield Strength (.2%) | σ­­YS | 2250 ± 210 MPa | 2220 ± 170 MPa
Compressive strength | σ­­UTS | 2670 ±139 MPa | 2620 ± 200 MPa
Flexural Strength | σ­­b | 610 ± 130 MPa | 600 ± 78 MPa
Fracture Toughness* | KIC | 15.2 ± 1.1 MPa·m1/2 | 17.3 ± 2.2 MPa·m1/2
Residual Stress (TiC phase) |  | 148 MPa ± 35 MPa (compressive) | 285 MPa (compressive)
Density = 5,500 kg/m3
Much higher specific modulus and strength c.f. titanium alloys

## Slide 22
Comparisons

## Slide 23
SHS -TiC-Ni cermet (15vol% Ni)
SPS - TiC-Ni cermet (15vol% Ni)
Hardness = 16.5 GPa: sYS ~3.4 GPa
Hardness = 13.3 GPa: sYS ~2.7 GPa
Ti-TiB density =4,400 kgm-3
Ultra-strong (hard) materials
TiB
a Ti
TiC
NiMo
Adapted from Compton and Zok
TiC
NiMo
SPS - TiB2 +15vol%Ti
1650oC 10min 50MPa
Hardness = 25.2 GPa

## Slide 24
CNT/BMI
Carbon nanotube composites
Wang et al Mater. Res. Lett 2013
CNT/BMI
Other ways to play the nano card?

## Slide 25
FCC metals
Covalent solids
Opportunity to create metallic nanolattice that is 10X stronger than SOA at 5 nm.
But ceramics offer transformational opportunities at 0.5 mm strut diameter.
Silicon carbide
Shin et al 2012
Nickel inverse opal with 20 nm width ligaments
Relative density=10%
Density=0.1x3,200 kgm-3 = 320 kgm-3
a-SiC Syntatic foam
The Theoretical Strength of Nanoscopic Materials

## Slide 26
Increased strength of pillars as pillar diameter decreased due to reduction in sample volume (reduced probability of grain boundary flaws).
High strength at sub-micron scale results from initiation of <110>{111} slip
3C SiC (zinc blend structure)
Yield stress = 12-15 GPa

## Slide 27
Examples of other size dependent properties
Catalytic properties –nano-materials have enhanced chemical reaction rates (endothermic reactions with jet fuel)
Electrochemical properties – nano-materials rapidly transfer ions (Li+ ion rechargeable batteries)
Melting properties – nano-materials have lower transition temperatures from solid to liquid (thermal batteries)
Magnetic properties – nano allows control of the electron spin interactions (magnetic flow control)
Optical properties – nanomaterials enable novel uses of light (transparency, electrochromics)
Wetting –radius of curvature changes liquid surface contact angle (super hydrophobicity- novel heat transfer)
Theoretical strength limit reached at small size
Nano-octet lattice strength
Example of a hierarchical lattice
t
Lattices Assembled From Nanoscopic Materials That Reach Their Theoretical Strength
Struts approach
the strength limit size
FCC Example: Copper
Copper
Covalent Example : SiC
Julia Greer (Caltech)
http://www.nanoscribe.de/en/

## Slide 28: Scaling laws for the strength and toughness of a stretch dominated lattice
Yield strength
of lattice
Yield strength
of parent solid
density of lattice
density of parent solid
Fracture toughness
of lattice
Cell size
Failure strain
yield strain
The Ti-6Al-4V alloy example
=1000 MPa
= 4.5 Mgm-3
= 0.45 Mgm-3
Hence,
=100 MPa
for = 1-10mm
Fleck et al 2010

## Slide 29
There may be a solution,.. consider crack propagation in hierarchical lattices
Consider the propagation of a crack through a lattice itself made of a nano-lattice (or foam) of a single small cell size.
When the crack tip is in a large cell
When the crack tip is in a small cell
For Lo >> lo , and the crack arrests between the large cell size struts, resulting in high fracture toughness.
Say 5 mm
Say 20 nm
Octet lattice made from an
inverse opal

## Slide 30
Hierarchical Light Lattices (Half Density of Water)
Inverse opal
Inverse opal
IO from IO
Octet from inverse opal
Octet lattice made from an
inverse opal

## Slide 31
Hierarchical SiC Lattices: Inverse opal nanolattice vs 3D printed lattice
Assume 30% relative density for the large cell octet lattice
Strength of Octet-Octet 3D printed lattice:
Strength of Inverse Opal-Octet hierarchical lattice:
0.3 x 3,200 kgm-3 = 960 kgm-3
Octet from inverse opal
10 mm
5 mm

## Slide 32
The Strength and Toughness Predictions for Lattices with a Density a Half Density of Water
Only tan colored bubbles have density < water
Ceramic options have high strength/toughness at low density + multifunctionality
New opportunity?
Integrated Computational Materials Engineering
(exploits MGI)
Computational modeling of functional properties can be used to discover/invent new hierarchical hybrids with revolutionary combinations of materials functionalities.
+
Simulation/control of microstructure evolution (material states) during synthesis and processing
Silicon carbide
Inverse opal
Inverse opal
IO from IO
Octet from inverse opal

## Slide 33
The Emerging Hierarchical Lattices Opportunity
Combine newly developed capabilities with manufacturing, materials (genomic) modelling, multiscale topology optimization that create new states of matter with compelling multifunctionalities for NASA applications
Example functionalities
Mechanical structure + energy storage (thermal via phase change, endothermic reactions, ion diffusion)
+ Heat transfer (two phase, magnetic control)
+ Signature control (acoustic, E/M damping, IR frequency control, electrochromic displays)
nano and macro lattice lengths scales + materials selection + novel integration strategies = new design paradigm
Applications

## Slide 34
Concluding Remarks
Stretching governed (high nodal connectivity) lattices have moduli approaching material limits. Modulus is topology dependent and proportional to that of the solid and relative density.
Their strength is well predicted by models but today’s materials remains are well below theoretical limits.
The strength of octet lattices can be increased using lightweight materials:
  Metal bonded ceramics
  Nanoscopic (defect starved) struts (nanolattices/inverse opals)
  CFRP struts with very high matrix shear strength (CNT or BNCT – eventually graphene reinforced)
  But their toughness is predicted to be (very) low.
Hierarchical lattices look promising for combining strength and toughness, and may exhibit numerous other functionalities (heat transfer, catalysis, energy storage).

## Slide 35
Fracture toughness predictions for 15wt%Ti-TiB2 octet truss lattice
Fracture toughness of octet truss lattice
Note, fracture toughness of a lattice structure is also given by
For an octet truss lattice, it is
Topology parameter S0.136
For Ti-6Al-4V octet truss lattice, ~ 10; for Ti-TiB2 cermet, ~1

## Slide 36
BUT,… crack propagation is easy in single cell size nano-lattices (or foams)
Consider a cellular lattice (or foam) structure with a single cell size characterized by a strut length lo.
Suppose it contains a flaw of length 2a
When the structure is loaded by applying a stress, at the sample boundaries,
the stress at the tip of the crack rises (intensifies) by a factor that increases with crack length and with decrease in the radius of curvature at the crack tip:
The crack tip radius of curvature is approximately the cell strut length. Thus the stress at the crack tip increases as the cell size decreases.
The resistance to crack extension decreases as cells get small – is very small for nanoscopic struts!

## Slide 37
b
c
d
Representative responses of SENB samples
Crack extension occurs by strut failure at low density and nodal fracture at higher density

## Slide 38
SiC inverse opal with ligaments <1 mm width
Relative density=50%
Density of SiC =3,200 kgm-3
Unpublished work of James Pikul (from his University Illinois web site)

## Slide 39
Ti octet lattice
Hierarchical lattices
Ti lattice is 3x stronger and tougher than isotropic woods
Tougher than light metals
Strong as steel
Octet lattice
Hierarchical octet lattice
Program has developed a titanium octet lattice “super wood” that 3x stronger and 3-30x tougher than isotropic wood.
Multi-kg scale fabrication demonstrated.
Micromechanical analysis indicates that if the Ti struts of the lattice are replaced by microlattice made from high elastic modulus struts (whose strength approaches material theoretical limits) a hierarchical lattice can be made.
HL’s would be tougher than light metals, stronger than many steels But have a density less than water!
+
Multifunctionality
Lattices also exhibit multifunctionality
Efficient cross flow heat exchange
Acoustic metamaterials (stop bands)
Controllable m-wave reflectivity
Shape morphing structures
Novel batteries
Silicon Carbide Hierarchical Lattices with Light Metal Toughness and Nickel Alloy Strength
Many processing routes

## Slide 40
Predictions for lattices with a density = 500 kg m-3
Materials in blue have a density >500 kgm-3
Only tan and pink have required density
Natural woods are highly anisotropic.
Isotropic wood*
Can a titanium octet lattice really do better than “isotropic” (MDF) wood?
Upper bound toughness predictions
*Medium density fiber board (MDF)

## Slide 42
σc = 3248 MPa± 313MPa
σf = 262 MPa ± 22MPa
Compressive strength
Flexural strength
Fracture surface after 4 points bending
Hardness
H = 25GPa
SPS 15wt%Ti-TiB2: Hot pressed 1650C 15min 50MPa

## Slide 43
A simple “snap-fit” fabrication approach and szz pyramidal lattice compression results
FEM results use σc= 2600 and 3300 MPa material models for FEM min and max predictions.

## Slide 44
A conservative compressive strength of 2600MPa was used for the analytical model predictions. 2600 and 3300 MPa material’s models were used for the minimum and maximum FE predictions
Predictions and measurements of compressive modulus and strength

## Slide 47: Microlattice with microscale octet unit cells
Z =12
Zheng et al., Science, June 2014, Vol. 344, 6190

## Slide 48: Ultralight lattices with an array of material constituents across large density range can be constructed
Lattice materials with density range across five orders of magnitude have been created
Notes: We fabricated the octet lattice materials into standard face centered cubic lattices of the same sizes to characterize this materials
material constituent ranging from polymer, to metal and ceramic.
two configurations, solid and hollow, with densities ranging across five orders of magnitude from as large as hundreds of kg.cm-3 as light as 1 kg.cm-3

## Slide 49: Multiscale metallic metamaterials --- across over 7 orders of magnitude in length-scale
Zheng et al., Nature Materials, 2016 In Press

## Slide 50
Net Shape TiB2Ti Trusses
1
2
3
50 MPa

## Slide 51
Fracture toughness predictions for 15wt%Ti-TiB2 octet truss lattice
Fracture toughness of octet truss lattice
Note, fracture toughness of a lattice structure is also given by
For an octet truss lattice, it is
Topology parameter S0.136
For Ti-6Al-4V octet truss lattice, ~ 10; for Ti-TiB2 cermet, ~1